## Slide 1
Electrospun Silk-Boron Nitride Nanofibers with Tunable Structure and Properties
Polymers 2020
Course overview
h-BN changes the morphology, secondary structure and thermal stability of electrospun silk fibers, making them more tunable for biofriendly composite use.
Source
https://www.mdpi.com/2073-4360/12/5/1093

## Slide 2
汇报提纲
Outline
1. 问题与动机 2. 发展脉络 3. 方法对比 4. 本文方法 5. 实验结果 6. 局限与展望

## Slide 3
研究背景
Why it matters
Electrospun silk can be made into porous mats, but its thermal and structural stability still needs help.
Main bottleneck
A filler must reinforce the protein matrix without destroying processability.
Core idea
Use h-BN nanosheets to tune fiber morphology, crosslinking and protein secondary structure.

## Slide 4
发展脉络
Timeline
2003 · Electrospinning matures — Fiber morphology becomes controllable by process tuning. 2010 · Silk biomaterials — Silk expands into scaffolds, dressings and devices. 2015 · BN thermal fillers — BN becomes a major electrically insulating conductor filler. 2020 · Silk-BN fibers — The paper maps how BN changes fiber structure and stability.

## Slide 5
Benchmark 对比
Method | Strengths | Weaknesses
Pure SF nanofibers | Smooth and biofriendly | Limited thermal robustness
Low-BN BNSF | Better alignment | Modest reinforcement
High-BN BNSF | Rougher but more coupled | Excess loading may hurt texture
This work | Tunable electrospun biohybrid | No direct conductivity target reported

## Slide 6
方法流程
1. Dissolve silk
Prepare a formic-acid based spinning dope.
2. Add BN
Mix h-BN at different loading ratios.
3. Electrospin
Form composite fibers with tunable diameter and packing.
4. Characterize
Use SEM, FTIR, TGA and TM-DSC to map structure-property changes.

## Slide 7
核心公式与机理
Formula
Thermal stability is tracked by Tw, Tg and Td shifts after BN addition.
Interpretation
Tw — bound-water evaporation feature Tg — glass transition temperature Td — thermal degradation feature Diameter — morphology marker for electrospun mats

## Slide 8
核心结果
800 nm
approx. diameter of pure SF fibers
400-750 nm
diameter range after BN addition
120 °C
pure SF onset Tg
96 °C
lowest Tg at 40% BN

## Slide 9
相对表现
Pure SF Tg
40% BNSF Tg
Residual mass
Morphology control

## Slide 10
实验与验证
Method validation
Structure, thermal and cooling behavior are all checked.
Indoor tests
Simulated skin and wearable scenarios are used.
Outdoor tests
Sunlight or environment are incorporated when relevant.
Stability
Cycle, wetting or degradation are quantified.

## Slide 11
Mechanism
Heat transfer
The filler network changes phonon pathways and heat spreading.
Interface control
Surface chemistry decides whether the network remains useful.

## Slide 12
Key numbers to remember
Metric | Value | Meaning
Main thermal metric | 800 nm | approx. diameter of pure SF fibers
Secondary metric | 400-750 nm | diameter range after BN addition
Cooling metric | 120 °C | pure SF onset Tg
Durability / window | 96 °C | lowest Tg at 40% BN

## Slide 13
Application scenarios
Skin contact
Wearable patches and body surface cooling.
Bioelectronics
Heat removal from LEDs or soft devices.
Textiles / films
Large-area passive heat management.
Reusable settings
Washing, cycling or reuse depending on the paper.

## Slide 14
局限与展望
Current limitations
- The paper emphasizes structure tuning more than conductivity benchmarking. - Higher loading can roughen the fibers. - Biomedical validation remains prospective.
Future work
- Measure conductivity and anisotropy explicitly in aligned mats. - Link morphology tuning to cell response in wet environments. - Explore post-spinning annealing or stretching to amplify ordering. - Combine BN with additional benign fillers for multifunctionality.

## Slide 15
总结
Summary
h-BN changes the morphology, secondary structure and thermal stability of electrospun silk fibers, making them more tunable for biofriendly composite use. The main design principle is to align filler geometry, interfacial chemistry and matrix choice with the target cooling mode. Source: https://www.mdpi.com/2073-4360/12/5/1093

## Slide 16
References
DOI
10.3390/polym12051093
Article page
https://www.mdpi.com/2073-4360/12/5/1093