## Slide 1
High Thermal Conductivity and Radiative Cooling Designed Boron Nitride Nanosheets/Silk Fibroin Films for Personal Thermal Management
ACS Applied Materials & Interfaces 2024
Course overview
BNNS and silk fibroin are combined into an aligned, reusable cooling film that balances heat spreading, radiative cooling and skin compatibility.
Source
https://pubs.acs.org/doi/10.1021/acsami.3c16602

## Slide 2
汇报提纲
Outline
1. 问题与动机 2. 发展脉络 3. 方法对比 4. 本文方法 5. 实验结果 6. 局限与展望

## Slide 3
研究背景
Why it matters
Cooling is energy intensive, so passive skin-contact cooling is a practical target.
Main bottleneck
Pure silk is biocompatible but not conductive enough for rapid heat dissipation.
Core idea
Use BNNS as a directional heat spreader and silk fibroin as a durable matrix.

## Slide 4
发展脉络
Timeline
2012 · Silk thermal transport — Silk becomes a serious thermal-material candidate. 2017 · BNNS composite films — Oriented BN starts to dominate in-plane heat flow. 2020 · Wearable passive cooling — Textiles and films converge for body cooling. 2024 · BNNS/SF film — The paper integrates alignment, reflectance and biocompatibility.

## Slide 5
Benchmark 对比
Method | Strengths | Weaknesses
Pure SF | Biobased and flexible | Thermal transport is too low
Graphene textiles | Good conduction | Wearability and outdoor cooling tradeoffs
BNNS polymer films | Strong anisotropic heat spreading | Less skin-friendly matrix
BNNS/SF film | Aligned, reusable, biocompatible | High filler loading may reduce softness

## Slide 6
方法流程
1. Prepare BNNS
Exfoliate h-BN into nanosheets without losing the platelet structure.
2. Mix with SF
Combine with silk fibroin before vacuum filtration.
3. Build alignment
Layer-by-layer stacking forms a directional thermal path.
4. Validate
Measure thermal conductivity, reflectance, emissivity and biosafety.

## Slide 7
核心公式与机理
Formula
λ = α × ρ × Cp; TCE = (λcomposite - λSF) / λSF × 100%
Interpretation
λ — effective thermal conductivity α — thermal diffusivity ρ — density Cp — specific heat capacity

## Slide 8
核心结果
27.58 W m−1 K−1
in-plane thermal conductivity
1.77 W m−1 K−1
out-of-plane thermal conductivity
0.89
solar reflectance
0.84
LWIR emissivity

## Slide 9
相对表现
Pure SF
BNNS/SF 50 wt%
Indoor cooling
Outdoor cooling

## Slide 10
实验与验证
Method validation
Structure, thermal and cooling behavior are all checked.
Indoor tests
Simulated skin and wearable scenarios are used.
Outdoor tests
Sunlight or environment are incorporated when relevant.
Stability
Cycle, wetting or degradation are quantified.

## Slide 11
Mechanism
Heat transfer
The filler network changes phonon pathways and heat spreading.
Interface control
Surface chemistry decides whether the network remains useful.

## Slide 12
Key numbers to remember
Metric | Value | Meaning
Main thermal metric | 27.58 W m−1 K−1 | in-plane thermal conductivity
Secondary metric | 1.77 W m−1 K−1 | out-of-plane thermal conductivity
Cooling metric | 0.89 | solar reflectance
Durability / window | 0.84 | LWIR emissivity

## Slide 13
Application scenarios
Skin contact
Wearable patches and body surface cooling.
Bioelectronics
Heat removal from LEDs or soft devices.
Textiles / films
Large-area passive heat management.
Reusable settings
Washing, cycling or reuse depending on the paper.

## Slide 14
局限与展望
Current limitations
- Very high filler loading may reduce softness. - Large-area alignment is harder to scale. - Wear, sweat and washing need broader field testing.
Future work
- Optimize interfacial chemistry to reduce phonon scattering. - Develop roll-to-roll or other scalable alignment routes. - Test laundering and fatigue under realistic clothing conditions. - Co-design with textile architectures for all-day comfort.

## Slide 15
总结
Summary
BNNS and silk fibroin are combined into an aligned, reusable cooling film that balances heat spreading, radiative cooling and skin compatibility. The main design principle is to align filler geometry, interfacial chemistry and matrix choice with the target cooling mode. Source: https://pubs.acs.org/doi/10.1021/acsami.3c16602

## Slide 16
References
DOI
10.1021/acsami.3c16602
Article page
https://pubs.acs.org/doi/10.1021/acsami.3c16602