## Slide 1
High Thermal Conductivity and Biocompatibility Silk Fibroin Hydrogels Filled with CDs@BNOH for Body Surface Cooling
ACS Applied Materials & Interfaces 2025
Course overview
Carbon-dot-modified hydroxylated BN is embedded into a silk hydrogel patch to balance thermal conduction, UV handling, biodegradability and skin-contact cooling.
Source
https://pubs.acs.org/doi/10.1021/acsami.5c09260

## Slide 2
汇报提纲
Outline
1. 问题与动机 2. 发展脉络 3. 方法对比 4. 本文方法 5. 实验结果 6. 局限与展望

## Slide 3
研究背景
Why it matters
Wearable cooling needs a matrix that is biocompatible, degradable and thermally useful.
Main bottleneck
Many conductive fillers are good conductors but poor skin-contact materials without surface engineering.
Core idea
Hydroxylated BN is further modified by carbon quantum dots to improve phonon transport and UV response.

## Slide 4
发展脉络
Timeline
2020 · Wearable passive cooling — Hydrogels and textiles begin to merge with cooling goals. 2022 · Biocompatible gels — Skin-contact materials become a major design target. 2024 · BNNS/SF cooling films — Film-type alignment and radiative cooling are proven. 2025 · CDs@BNOH/SilMA — This work adds surface engineering and degradable hydrogel integration.

## Slide 5
Benchmark 对比
Method | Strengths | Weaknesses
Commercial H2O@PAAS patch | Simple and available | Depends heavily on evaporation
Pure SilMA hydrogel | Soft and biobased | Thermal conductivity is modest
BNOH/SilMA | Better conduction than pure gel | Less interface engineering
CDs@BNOH/SilMA | Best balance here | Long-term wear still needs more data

## Slide 6
方法流程
1. Prepare CDs
Make carbon quantum dots from urea/citrate precursors.
2. Build CDs@BNOH
Functionalize hydroxylated BN with CDs to tune the interface.
3. Make SilMA
Methacrylate-modify silk fibroin for UV-curable gelation.
4. Infuse patch
Load the filler into cotton-supported gel and cure into a wearable patch.

## Slide 7
核心公式与机理
Formula
Proper CDs modification improves phonon transport; too much coating disrupts the BN network.
Interpretation
fwhm — Raman linewidth used as a phonon-lifetime indicator D% — degradation fraction of the hydrogel ΔT — surface cooling effect relative to blank λ — patch thermal conductivity

## Slide 8
核心结果
0.77 W m−1 K−1
patch thermal conductivity
15.38%
overall conductivity increase
6.6 °C
cooling improvement vs. control
10 °C+
indoor scenario peak cooling effect

## Slide 9
相对表现
BNOH/SilMA
CDs@BNOH/SilMA
Commercial patch
UV shielding

## Slide 10
实验与验证
Method validation
Structure, thermal and cooling behavior are all checked.
Indoor tests
Simulated skin and wearable scenarios are used.
Outdoor tests
Sunlight or environment are incorporated when relevant.
Stability
Cycle, wetting or degradation are quantified.

## Slide 11
Mechanism
Heat transfer
The filler network changes phonon pathways and heat spreading.
Interface control
Surface chemistry decides whether the network remains useful.

## Slide 12
Key numbers to remember
Metric | Value | Meaning
Main thermal metric | 0.77 W m−1 K−1 | patch thermal conductivity
Secondary metric | 15.38% | overall conductivity increase
Cooling metric | 6.6 °C | cooling improvement vs. control
Durability / window | 10 °C+ | indoor scenario peak cooling effect

## Slide 13
Application scenarios
Skin contact
Wearable patches and body surface cooling.
Bioelectronics
Heat removal from LEDs or soft devices.
Textiles / films
Large-area passive heat management.
Reusable settings
Washing, cycling or reuse depending on the paper.

## Slide 14
局限与展望
Current limitations
- Conductivity is still below the best film-type BNNS systems. - Outdoor performance depends on contact and ambient conditions. - Long-term wear tests are still limited.
Future work
- Quantify comfort under sweat, motion and repeated bending. - Optimize CDs loading to keep the BN phonon network intact. - Explore device integration for wearable electronics. - Test other biodegradable matrices and patch geometries.

## Slide 15
总结
Summary
Carbon-dot-modified hydroxylated BN is embedded into a silk hydrogel patch to balance thermal conduction, UV handling, biodegradability and skin-contact cooling. The main design principle is to align filler geometry, interfacial chemistry and matrix choice with the target cooling mode. Source: https://pubs.acs.org/doi/10.1021/acsami.5c09260

## Slide 16
References
DOI
10.1021/acsami.5c09260
Article page
https://pubs.acs.org/doi/10.1021/acsami.5c09260